Department of Technical Education

State Board of Technical Education &Training (TS)

| Course Title: | Material Testing Lab-II |  | Course Code : | CE-406 |
| --- | --- | --- | --- | --- |
| Semester: |  | IV Semester | Course Group : | Practical |
| Teaching Scheme in Periods(L:T:P): |  | 15:0:30 | Credits : | 2 |
| Methodology : |  | Lecture+ Practical | Total Contact Periods : | 45 |
| CIE : |  | 60 Marks | SEE : | 40 Marks |

Pre requisites

This course requires the knowledge of Construction Materials, Strength of materials, Reinforced Cement Concrete, Transportation Engineering, Soil mechanics and IS 383.

Course Outcomes

Upon the completion of the course, the student shall be able to

| CO1 | Adapt suitable sample of material and Identify standard equipment for conducting different tests based on standards of BIS |
| --- | --- |
| CO2 | Examine the suitability of Coarse aggregates for use in different construction and pavement works as per standards of BIS |
| CO3 | Analyze the data obtained from the tests of sieve analysis of soils and Field density of soils as per standards of BIS |
| CO4 | Correlate the soil properties as per Atterberg limits and Proctor compaction test as per standards of BIS |
| CO5 | Develop the concrete mix and examine the workability of fresh concrete as per standards of BIS |
| CO6 | Prepare Concrete specimens (cubes and cylinders) and perform the split tensile strength, Compressive strength. |

Course Content and Blue Print of Marks for SEE

| Unit No | Unit Name | Periods |
| --- | --- | --- |
| 1 | Tests on Aggregates | 15 |
| 2 | Tests on soils | 15 |
| 3 | Tests on Concrete | 15 |
| Total |  | 45 |

Course Contents

UNIT 1: Tests on Aggregates			Duration: 15 Periods (L:5 – P:10)

- Impact value of Coarse aggregate

- Crushing value of Coarse aggregate

- Abrasion Value of Coarse Aggregate

- Flakiness index of Coarse aggregate

- Elongation Index of Coarse aggregate

UNIT2: Tests on Soils				Duration: 15 Periods(L:5 – P:10)

- Sieve analysis of soil-Dry Method

- Field density of soil by sand replacement method

- Liquid Limit and Plastic Limit (Atterberg’s Limits)

- Proctor Compaction Test

UNIT 3: Tests on Concrete				Duration: 15 Periods(L:5-P:10)

- Workability by slump cone test.

- Workability by compaction factor test

- Casting and Testing of Cement concrete cubes for compressivestrength

- Non-destructive test on hardened concrete-Rebound Hammer test only

KEY Competencies to be achieved by the student

| S. No | Experiment Title | Key Competency |
| --- | --- | --- |
| 1 | Impact Value of Coarse aggregate IS 2386 Part-IV clause 4 | 1.Preparation of sample |
|  |  | 2.Weighing sample accurately |
|  |  | 3.Application of load by number of strokes carefully |
|  |  | 4. Weighing residue accurately |
| 2 | Crushing value of Coarse aggregate IS 2386 Part-IV clause 2 | 1.Preparation of sample |
|  |  | 2.Weighing sample accurately |
|  |  | 3.Application of load at required rate to the required period accurately |
|  |  | 4. Weighing of residue |
| 3 | Abrasion value of coarse aggregate IS 2386 Part-IV clause 5 | 1. Adopt the required abrasive value as per sample chosen |
|  |  | 2. Weighing sample accurately |
|  |  | 3.Counting the required number of rotations |
|  |  | 4. Weighing the residue |
| 4 | Flakiness Index of coarse aggregate IS 2386 Part-I clause 4 | 1.Correct arrangement of sieves used for the sieve analysis of coarse aggregate |
|  |  | 2. Collect and measure the aggregate sample |
|  |  | 3.Weighing of aggregate passing through thickness gauge correctly |
| 5 | Elongation Index of coarse aggregate IS 2386 Part-I clause 5 | 1.Correct arrangement of sieves used for the sieve analysis of coarse aggregate |
|  |  | 2. Collect and measure the aggregate sample |
|  |  | 3.Weighing of aggregate retained through length gauge correctly |
| 6 | Sieve analysis of Soil IS 2386 Part-I clause 2 | 1.Correct arrangement of sieves used for the sieve analysis of soil |
|  |  | 2.Weighing of residue in each sieve accurately |
|  |  | 3. Draw the semi log graph of grain distribution |
|  |  | 4. Correlate the D10, D30 and D60 |
| 7 | Field density of soil by Sand Replacement Method IS 2720 Part-28 | 1.Calibrate the apparatus accurately |
|  |  | 2. Weigh the samples accurately |
|  |  | 3.Calculate the density accurately |
| 8 | Attenbergs Limits IS 2720 Part-5 & IS 2720 Part- 6 | 1. Collecting required sample of soil |
|  |  | 2.Placing of required sample of soil in Casagrande’s apparatus in correct position |
|  |  | 3.Recording the number of drops to close the grove |
|  |  | 4. Removing sample for determining water content |
|  |  | 5.Rolling the sample on a glass plate to required diameter |
|  |  | 6. Collecting the sample for determining water content |
| 9 | Proctor’s Compaction Test IS 2720 Part-7 | 1.Weigh the soil accurately |
|  |  | 2.determine the water content accurately |
|  |  | 3. Apply required number of blows of compaction accurately |
|  |  | 4. correlate the observations to obtain the maximum dry density and optimum moisture content |
| 10 | Workability by Slump Cone Test IS 7320, IS1199 part 2& IS 456 | 1. Weigh the material accurately and mix the sample materials |
|  |  | 2. Placing in the slump cone |
|  |  | 3.Apply required number of tamping’s for each layer of concrete |
|  |  | 4. Measure the slump accurately |
| 11 | Compaction Factor test on Concrete IS 5515, 1199 part 2 & IS 456 | 1. Weigh the material accurately |
|  |  | 2.Weigh the mould and concrete accurately |
|  |  | 3. Calculate the compaction factor correctly |
| 12 | Casting of Cement Concrete Cubes IS 516 & IS 10086 | 1.Weigh the material accuratelyand mix the sample materials |
|  |  | 2.Vibrate the concrete filled in moulds to the required time correctly |
|  |  | 3. Cure the demoulded cubes to the required period |
| 13 | Testing of cement concrete cubes for compressive strength IS 516 clause 5 | 1.Apply the load at required rate correctly |
|  |  | 2. Record the load at failure correctly |
|  |  | 3. Calculate the compressive strength accurately |
| 14 | Non-Destructive test (Rebound Hammer Test) | 1.Place the rebound hammer in the correct direction |
|  |  | 2.Calculate the strength from the corresponding graph |

Recommended Books

            - Laboratory manual on Testing of Engineering Materials by HemantSood,New Age International Publishers,New Delhi

            - Building and Construction materials Testing and Quality Control by M.L.Gambhir and NehaJamwal,McgrawHill,India

            - Material Testing Laboratory manual by C.B.Kukreja, Kishore.K and Ravi Chawla,Standard Publishers Distributors

            - Concrete technology by M.S. Shettyand A. K. Jain

            - A Laboratory Manual on Soil Mechanics by Ravi Kumar Sharma

            - Highway materials and surface testing by B.L.Gupta&Amitgupta

Suggested E-learning references

- http://nptel.ac.in

- https://docslide.us/documents/som-bmt-lab-manual-final.html

- http://www.nitttrchd.ac.in/sitenew1/nctel/civil.php

- https://ts-nitk.vlabs.ac.in/List%20of%20experiments.html

- https://smfe-iiith.vlabs.ac.in/List%20of%20experiments.html

- https://cs-iitd.vlabs.ac.in/List%20of%20experiments.html

Suggested Learning Outcomes

Upon completion of the course, the student shall be able to

CO1 -Adapt suitable sample of material and Identify standard equipment for conducting different tests based on standards of BIS

CO2 - Examine the suitability of Coarse aggregates for use in different construction and pavement works as per standards of BIS

  - Study the significance of impact value of aggregate used for road construction

  - State the standards on impact value of aggregate used for various civil engineering works

  - Use the apparatus required for conducting impact test on aggregate

  - State the procedure for preparing the sample and no of samples required for the given work

  - Explain the procedure for conducting impact test on aggregate

  - Perform impact test on agiven sample of coarse aggregate

  - Draw inferences by conducting impact test on different types of natural aggregate

  - Study the significance of thecrushing value of aggregate used for various civil engineering works

  - State the standards for crushing value of aggregate used for various civil engineering works

  - Use the apparatus required for conducting thecrushing test on aggregate

  - State the procedure for preparing the sample and no of samples required for the given work

  - Explain the procedure for conducting thecrushing test on aggregate

  - Perform crushing test on agiven sample of coarse aggregate

  - Draw inferences by conducting thecrushing test on different types of natural aggregate

  - Study the significance of theabrasion value of aggregate used for road construction

  - State the standards on theabrasion value of aggregate used for various civil engineering works

  - Use the apparatus required for conducting theabrasion test on aggregate

  - State the procedure for preparing the sample and no of samples required for the given work

  - Explain the procedure for conducting theabrasion test on aggregate

  - Perform abrasion test on given sample of coarse aggregate

  - Draw inferences by conducting abrasion test on different types of natural aggregate

  - State the significance of flakiness index of aggregate on strength and workability properties of concrete

  - State the standards of flakiness index of aggregates

  - Explain the procedure and calculate the flakiness index for given sample of coarse aggregate

  - State the significance of elongation index of aggregate on strength and workability properties of concrete

  - State the standards of elongation index of aggregate

  - Explain the procedure and calculate the elongation index of given sample of coarse aggregate

CO3 - Analyze the data obtained from the tests of sieve analysis of soils and Field density of soils as per standards of BIS

CO4 - Correlate the soil properties as per Atterberg limits and Proctor compaction test as per standards of BIS

  - Study the classifications of various types of soils

  - Use theapparatus required for conducting sieve analysis of soils

  - Explain the procedure for conducting sieve analysis of soils

  - Perform sieve analysis over a given soil sample

  - Study the significance of field density of soil

  - Use the apparatus required for conducting field density of soil

  - Explain the procedure for conducting field density test on thesoil by sand replacement method

  - Calculate the field density of agiven sample of soil by sand replacement method

  - Study the significance of Atterberg’s limits of soil in Civil Engineering activities

  - Use apparatus required for conducting tests to determine Atterberg limits of soil

  - Explain the procedure for finding Atterberg’s limits of soil

  - Perform tests to determine liquid the limit, Plastic limit and Shrinkage limit of a given soil sample

  - Calculate the values of Atterberg limits of a given soil sample from the observation of tests

  - Study the significance of the proctor compaction test

  - Use the apparatus required for conducting the proctor compaction test

  - Explain the procedure for conducting the proctor compaction test

  - Conduct the proctor compaction test for a given sample of soil

  - Compare the observations of tests conducted on different types of soils

  - Draw the graph for proctor’s compaction test

  - Calculate the values of OMC and MDD of given soil sample from the observations of the test

CO5 - Develop the concrete mix and examine the workability of fresh concrete as per standards of BIS

CO6 - Prepare Concrete specimens (cubes and cylinders) and perform the split tensile strength, Compressive strength.

  - State the importance of workability on strength properties of concrete

  - State various types of tests used for measuring the workability of fresh concrete

  - State standards of workability of concrete used for different places of construction work

  - Explain and perform slump test of workability on fresh concrete for given ingredients

  - Draw inference from test results on slump test on workability of concrete made with Coarse aggregate having different elongation index

  - Draw inference from test results on slump test on workability of concrete made with Coarse aggregate having different flakiness index

  - Compare the slumps of concrete made with gap-graded coarse aggregate and well-graded coarse aggregate

  - State the purpose of compaction of concrete

  - Explain and Perform compaction factor test of workability on fresh concrete for given ingredients

  - Draw inference from test results on compaction factor test of workability of concrete made with coarse aggregate having different elongation index values

  - Draw inference from test results on compaction factor test of workability of concrete made with coarse aggregate having different flakiness index values

  - Compare the compaction factors of concrete made with gap-graded coarse aggregate and that made with well-graded coarse aggregate

  - Study the purpose of casting concrete cubes

  - Use equipment required for the casting of cement concrete cubes

  - Explain the procedure for casting concrete cubes

  - Cast the concrete cubes with given ingredients

  - State the importance of testing concrete cubes

  - Use equipment required for conducting compression test concrete cubes

  - State the precautions to be taken for testing concrete cubes

  - Explain the procedure for conducting compression test on concrete cubes

  - Draw inference from test results on compressive strength of concrete cubes Made with coarse aggregate having different elongation index values

  - Draw inference from test results on compressive strength of concrete cubes Made with coarse aggregate having different flakiness index values

  - Compare the compressive strengths of concrete cubes of concrete made with gap graded coarse aggregate and those made with well graded coarse aggregate

  - Compare the compressive strengths of concrete cubes of concrete made with Potable water and concrete cubes made and cured with non-potable water

  - State the importance of conducting NDT on concrete

  - Use the equipment on cement cubes and cement flooring in the correct direction

  - Calculate the compressive strength of concrete by using a rebound hammer.

Suggested Student Activities

- Collecting and study of various IS codes regarding testing of materials

- Testing of coarse aggregate used in pavement works in nearby vicinity.

- Tools and equipment used with pictorial presentation chart

- Collecting of various materials and correlate with standards.

- Study the methods of enhancing workability of concrete without using any admixtures.

- Collect different soils and conduct test for their properties.

- Study &Compare the compressive strength values of rebound hammer test and ultra-sonic pulse velocity tests

- Tech fest/Srujana

- Paper/Poster presentation

- Prepare a report on comparison of  Field density of soil by Sand Replacement         Method with Core cutter method

- Prepare a report on comparison of  Proctor Compaction Test with modified proctor compaction test

CO-PO Mapping Matrix

|  | Basic and Discipline Specific Knowledge | Problem Analysis | Design/Development of Solutions | Engineering Tools, Experimentation and Testing | Engineering Practices for Society, Sustainability and Environment | Project Management | Lifelong Learning | Linked PO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CO | PO1 | PO2 | PO3 | PO4 | PO5 | PO6 | PO 7 |  |
| CO1 | 2 | - | - | 2 | 1 | 2 | 2 | 1,4,5,6,7 |
| CO2 | 3 | - | 2 | 2 | 1 | 2 | 2 | 1,3,4,5,6,7 |
| CO3 | 3 | - | 2 | 2 | 1 | 2 | 2 | 1,3,4,5,6,7 |
| CO4 | 3 | 1 | 2 | 2 | 1 | 2 | 2 | 1,2,3,4,5,6,7 |
| CO5 | 3 | 1 | 2 | 2 | 1 | 2 | 2 | 1,2,3,4,5,6,7 |
| CO6 | 3 | 1 | 2 | 2 | 1 | 2 | 2 | 1,2,3,4,5,6,7 |

State Board of Technical Education and Training,Telangana

Mid Sem-I Model Question paper

DCE IV Semester

Course Code:CE-406					        Duration:1 hour

Course Name: Material Testing Lab-II		 Max.Marks:20 Marks

----------------------------------------------------------------------------------------------------------------

Instructions to the Candidate:

(i)Answer any One of the following Questions..Each question carries 20 marks

(ii) Check the suitability of the given construction material by drawing suitable inference

- Calculate the impact value of given sample of coarse aggregate

- Calculate the crushing value of given sample of coarse aggregate

- Calculate the abrasion value of given sample of coarse aggregate

- Calculate the flakiness index of given sample of aggregate

- Calculate the elongation index of given sample of aggregate

State Board of Technical Education and Training,Telangana

Mid Sem-IIModel Question paper

DCE IV Semester

Course Code:CE-406					        Duration:1 hour

Course Name: Material Testing Lab-II		     Max.Marks:20 Marks

----------------------------------------------------------------------------------------------------------------

Instructions to the Candidate:

(i)Answer any One of the following Questions.Each question carries 20 marks

(ii) Check the suitability of the given construction material by drawing suitable inference

- Draw the grading cure for the given sample of soil

- Calculate the field density of soil using sand replacement method

- Determine the liquid limit of the given soil sample

- Determine the plastic limit of the given soil sample

- Calculate the optimum moisture content and maximum dry density for the given sample using Proctor’s compaction test

State Board of Technical Education and Training,Telangana

Semester End Examination

Model Question paper

DCE IV Semester

Course Code:CE-509					        Duration:2 hours

Course Name: Material Testing Lab-II		  Max.Marks:40 Marks

----------------------------------------------------------------------------------------------------------------

Instructions to the Candidate:

(i)Answer any One of the following Questions.Each question carries 40 marks

(ii) Check the suitability of the given construction material by drawing suitable inference

- Calculate the impact value of given sample of coarse aggregate

- Calculate the crushing value of given sample of coarse aggregate

- Calculate the abrasion value of given sample of coarse aggregate

- Calculate the flakiness index of given sample of coarse aggregate

- Calculate the elongation index of given sample of coarse aggregate

- Calculate the field density of soil using sand replacement method

- Draw the grading curve for the given sample of soil

- Determine the liquid limit of the given soil sample

- Determine the plastic limit of the given soil sample

- Calculate the optimum moisture content and maximum dry density for the given sample using Proctor’s compaction test

- Determine workability of the fresh concrete prepared with the given mix proportion and water cement ratio using slump test

- Determine the compaction factor of the fresh concrete prepared with the given mix proportion and water cement ratio using compaction factor test.

- Prepare three sample concrete cubes with the given mix proportion and water cement ratio

- Calculate the compressive strength of the given cement concrete cubes

- Calculate the Strength of any concrete structure in your college, using Rebound Hammer method.