Department of Technical Education

State Board of Technical Education &Training (TS)

| Course Title: | Concrete Technology lab |  | Course Code : | CE-406 |
| --- | --- | --- | --- | --- |
| Semester: |  | IVSemester | Course Group : | Practical |
| Teaching Scheme in Periods(L:T:P): |  | 15:0:30 | Credits : | 2 |
| Methodology : |  | Lecture+ Practical | Total Contact Periods : | 45 |
| CIE : |  | 60 Marks | SEE : | 40 Marks |

Pre requisites

This course requires the knowledge of Building Materials and Construction Practice, Concrete Technology, Fundamentals of Reinforced Cement Concrete, Transportation Engineeringand IS codes.

Course Outcomes

Upon the completion of the course, the student shall be able to

| CO1 | Adapt suitable sample of material and Identifystandard equipment for conducting different tests based on standards of BIS |
| --- | --- |
| CO2 | Examine the suitability of Coarse aggregates for use in different construction and pavement works as per standards of BIS |
| CO3 | Examine the workability of fresh concrete as per standards of BIS |
| CO4 | Suitability of the concrete mix prepared per standards of BIS |
| CO5 | Prepare Concrete specimens (cubes and cylinders)and determine the Compressive strength. |
| CO6 | Performtheflexure and split tensile strength on different grades of concrete. |

Course Content and Blue Print of Marks for SEE

| Unit No | Unit Name | Periods |
| --- | --- | --- |
| 1 | Tests on Aggregates | 15 |
| 2 | Tests on soils | 15 |
| 3 | Tests on Concrete | 15 |
| Total |  | 45 |

Course Contents

UNIT 1: Tests on Aggregates			Duration: 15 Periods (L:5 – P:10)

- Impact value of Coarse aggregate

- Crushing value of Coarse aggregate

- Abrasion Value of Coarse Aggregate

- Flakiness index of Coarse aggregate

- Elongation Index of Coarse aggregate

UNIT2: Tests on Fresh Concrete			Duration: 15 Periods(L:5 – P:10)

- Workability by slump cone test.

- Workability by compaction factor test

- Workability by VEE – BEE test

- Workability by flow table test

UNIT 3: Tests on Hardened Concrete		Duration: 15 Periods(L:5-P:10)

- Casting and Testing of Cement concrete cubes for compressivestrength

- Casting and Testing of Cement concrete cylinders for compressivestrength

- Flexure Test

- Split Tensile Test

KEY Competencies to be achieved by the student

| S. No | Experiment Title | Key Competency |
| --- | --- | --- |
| 1 | Impact Value of Coarse aggregate IS 2386 Part-IV clause 4 | 1.Preparation of sample |
|  |  | 2.Weighing sample accurately |
|  |  | 3.Application of load by number of strokes carefully |
|  |  | 4. Weighing residue accurately |
| 2 | Crushing value of Coarse aggregate IS 2386 Part-IV clause 2 | 1.Preparation of sample |
|  |  | 2.Weighing sample accurately |
|  |  | 3.Application of load at required rate to the required period accurately |
|  |  | 4. Weighing of residue |
| 3 | Abrasion value of coarse aggregate IS 2386 Part-IV clause 5 | 1. Adopt the required abrasive value as per sample chosen |
|  |  | 2. Weighing sample accurately |
|  |  | 3.Counting the required number of rotations |
|  |  | 4. Weighing the residue |
| 4 | Flakiness Index of coarse aggregate IS 2386 Part-I clause 4 | 1.Correct arrangement of sieves used for the sieve analysis of coarse aggregate |
|  |  | 2. Collect and measure the aggregate sample |
|  |  | 3.Weighing of aggregate passing through thickness gauge correctly |
| 5 | Elongation Index of coarse aggregate IS 2386 Part-I clause 5 | 1.Correct arrangement of sieves used for the sieve analysis of coarse aggregate |
|  |  | 2. Collect and measure the aggregate sample |
|  |  | 3.Weighing of aggregate retained through length gauge correctly |
| 6 | Workability by Slump Cone Test IS 7320, IS1199 part 2& IS 456 | 1. Weigh the material accurately and mix the sample materials |
|  |  | 2. Placing in the slump cone |
|  |  | 3.Apply required number of tamping’s for each layer of concrete |
|  |  | 4. Measure the slump accurately |
| 7 | Compaction Factor test on Concrete IS 5515, 1199 part 2 & IS 456 | 1. Weigh the material accurately |
|  |  | 2.Weigh the mould and concrete accurately |
|  |  | 3. Calculate the compaction factor correctly |
| 8 | Casting of Cement Concrete Cubes IS 516 & IS 10086 | 1.Weigh the material accuratelyand mix the sample materials |
|  |  | 2.Vibrate the concrete filled in moulds to the required time correctly |
|  |  | 3. Cure the demoulded cubes to the required period |
| 9 | Testing of cement concrete cubes for compressive strength IS 516 clause 5 | 1.Apply the load at required rate correctly |
|  |  | 2. Record the load at failure correctly |
|  |  | 3. Calculate the compressive strength accurately |
| 10 | Testing of cement concrete cylinder for compressive strength IS 516 clause 5 | 1.Apply the load at required rate correctly |
|  |  | 2. Record the load at failure correctly |
|  |  | 3. Calculate the compressive strength accurately |
| 11 | Testing of cement concrete cubes for Flexural strength IS 516 clause 5 | 1.Apply load continuously without shock at a uniform rate until failure |
|  |  | 2. Record the maximum load at failure |
|  |  | 3. Calculate the Flexural strength |
| 12 | Testing of cement concrete cylinder forSplitting Tensile Strength of Concrete IS 5816 | 1.Apply the Load applied uniformly without shock until failure |
|  |  | 2. Record the maximum applied load |
|  |  | 3. Calculate the Split tensile strength calculated using IS formula |

Recommended Books

            - Laboratory manual on Testing of Engineering Materials by HemantSood,New Age International Publishers,New Delhi

            - Building and Construction materials Testing and Quality Control by M.L.Gambhir and NehaJamwal,McgrawHill,India

            - Material Testing Laboratory manual by C.B.Kukreja, Kishore.K and Ravi Chawla,Standard Publishers Distributors

            - Concrete technology by M.S. Shettyand A. K. Jain

            - A Laboratory Manual on Soil Mechanics by Ravi Kumar Sharma

            - Highway materials and surface testing by B.L.Gupta&Amitgupta

Suggested E-learning references

- http://nptel.ac.in

- https://docslide.us/documents/som-bmt-lab-manual-final.html

- http://www.nitttrchd.ac.in/sitenew1/nctel/civil.php

- https://ts-nitk.vlabs.ac.in/List%20of%20experiments.html

- https://smfe-iiith.vlabs.ac.in/List%20of%20experiments.html

- https://cs-iitd.vlabs.ac.in/List%20of%20experiments.html

Suggested Learning Outcomes

Upon completion of the course, the student shall be able to

CO1 -Adapt suitable sample of material and Identify standard equipment for conducting different tests based on standards of BIS

CO2 - Examine the suitability of Coarse aggregates for use in different construction and pavement works as per standards of BIS

  - Study the significance of impact value of aggregate used for road construction

  - State the standards on impact value of aggregate used for various civil engineering works

  - Use the apparatus required for conducting impact test on aggregate

  - State the procedure for preparing the sample and no of samples required for the given work

  - Explain the procedure for conducting impact test on aggregate

  - Perform impact test on agiven sample of coarse aggregate

  - Draw inferences by conducting impact test on different types of natural aggregate

  - Study the significance of thecrushing value of aggregate used for various civil engineering works

  - State the standards for crushing value of aggregate used for various civil engineering works

  - Use the apparatus required for conducting thecrushing test on aggregate

  - State the procedure for preparing the sample and no of samples required for the given work

  - Explain the procedure for conducting thecrushing test on aggregate

  - Perform crushing test on agiven sample of coarse aggregate

  - Draw inferences by conducting thecrushing test on different types of natural aggregate

  - Study the significance of theabrasion value of aggregate used for road construction

  - State the standards on theabrasion value of aggregate used for various civil engineering works

  - Use the apparatus required for conducting theabrasion test on aggregate

  - State the procedure for preparing the sample and no of samples required for the given work

  - Explain the procedure for conducting theabrasion test on aggregate

  - Perform abrasion test on given sample of coarse aggregate

  - Draw inferences by conducting abrasion test on different types of natural aggregate

  - State the significance of flakiness index of aggregate on strength and workability properties of concrete

  - State the standards of flakiness index of aggregates

  - Explain the procedure and calculate the flakiness index for given sample of coarse aggregate

  - State the significance of elongation index of aggregate on strength and workability properties of concrete

  - State the standards of elongation index of aggregate

  - Explain the procedure and calculate the elongation index of given sample of coarse aggregate

CO3 –Develop the concrete mix and examine the workability of fresh concrete as per standards of BIS

CO4- Suitability of the concrete mix for different applications in civil based on the various workability test

2.1 Study the concept and significance of workability of fresh concrete in construction practices.

2.2 Study the significance, standards, and applications of slump test for determining workability of fresh concrete.

2.3 Perform slump cone test on a given concrete sample and interpret different types of slump.

2.4 Study the significance of compaction factor test for low workability concrete and explain the test procedure.

2.5 Draw inferences on workability from compaction factor test results.

2.6 Study the significance of Vee–Bee test for very stiff concrete mixes and explain the test procedure.

2.7 Interpret Vee–Bee time to assess workability of concrete.

2.8 Study the significance of flow table test for high workability and flowing concrete.

2.9 Perform flow table test on a given concrete sample and draw inferences on workability.

CO5 - Develop the concrete mix and examine the workability of fresh concrete as per standards of BIS

CO6 - Prepare Concrete specimens (cubes and cylinders) and perform the split tensile strength, Compressive strength.

  - State the importance of workability on strength properties of concrete

  - State various types of tests used for measuring the workability of fresh concrete

  - State standards of workability of concrete used for different places of construction work

  - Explain and perform slump test of workability on fresh concrete for given ingredients

  - Draw inference from test results on slump test on workability of concrete made with Coarse aggregate having different elongation index

  - Draw inference from test results on slump test on workability of concrete made with Coarse aggregate having different flakiness index

  - Compare the slumps of concrete made with gap-graded coarse aggregate and well-graded coarse aggregate

  - State the purpose of compaction of concrete

  - Explain and Perform compaction factor test of workability on fresh concrete for given ingredients

  - Draw inference from test results on compaction factor test of workability of concrete made with coarse aggregate having different elongation index values

  - Draw inference from test results on compaction factor test of workability of concrete made with coarse aggregate having different flakiness index values

  - Compare the compaction factors of concrete made with gap-graded coarse aggregate and that made with well-graded coarse aggregate

  - Study the purpose of casting concrete cubes

  - Use equipment required for the casting of cement concrete cubes

  - Explain the procedure for casting concrete cubes

  - Cast the concrete cubes with given ingredients

  - State the importance of testing concrete cubes

  - Use equipment required for conducting compression test concrete cubes

  - State the precautions to be taken for testing concrete cubes

  - Explain the procedure for conducting compression test on concrete cubes

  - Draw inference from test results on compressive strength of concrete cubes Made with coarse aggregate having different elongation index values

  - Draw inference from test results on compressive strength of concrete cubes Made with coarse aggregate having different flakiness index values

  - Compare the compressive strengths of concrete cubes of concrete made with gap graded coarse aggregate and those made with well graded coarse aggregate

  - Compare the compressive strengths of concrete cubes of concrete made with Potable water and concrete cubes made and cured with non-potable water

  - State the importance of conducting NDT on concrete

  - Use the equipment on cement cubes and cement flooring in the correct direction

  - Calculate the compressive strength of concrete by using a rebound hammer.

Suggested Student Activities

- Collecting and study of various IS codes regarding testing of materials

- Testing of coarse aggregate used in pavement works in nearby vicinity.

- Tools and equipment used with pictorial presentation chart

- Collecting of various materials and correlate with standards.

- Study the methods of enhancing workability of concrete without using any admixtures.

- Study &Compare the compressive strength , flexure and split tensile strength values of  different concrete mixes

- Tech fest/Srujana

- Paper/Poster presentation

CO-PO Mapping Matrix

|  | Basic and Discipline Specific Knowledge | Problem Analysis | Design/Development of Solutions | Engineering Tools, Experimentation and Testing | Engineering Practices for Society, Sustainability and Environment | Project Management | Lifelong Learning | Linked PO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CO | PO1 | PO2 | PO3 | PO4 | PO5 | PO6 | PO 7 |  |
| CO1 | 1 | 1 | - | 2 | - | - | 1 | 1,2,4,7 |
| CO2 | 1 | 2 | - | 2 | - | - | 1 | 1,2,4,7 |
| CO3 | 1 | 2 | 1 | 3 | - | - | 1 | 1,2,3,4,7 |
| CO4 | 1 | 2 | 1 | 3 | - | - | 1 | 1,2,3,4,7 |
| CO5 | 2 | 2 | - | 3 | - | - | 1 | 1,2,4,7 |
| CO6 | 1 | 1 | 2 | 2 | - | - | 1 | 1,2,3,4,7 |

State Board of Technical Education and Training,Telangana

Mid Sem-I Model Question paper

DCTMIV Semester

Course Code:CE-406					        Duration:1 hour

Course Name:Concrete Technology Lab		 Max.Marks:20 Marks

----------------------------------------------------------------------------------------------------------------

Instructions to the Candidate:

(i)Answer any One of the following Questions..Each question carries 20 marks

(ii) Check the suitability of the given construction material by drawing suitable inference

- Calculate the impact value of given sample of coarse aggregate

- Calculate the crushing value of given sample of coarse aggregate

- Calculate the abrasion value of given sample of coarse aggregate

- Calculate the flakiness index of given sample of aggregate

- Calculate the elongation index of given sample of aggregate

State Board of Technical Education and Training,Telangana

Mid Sem-IIModel Question paper

DCTMIV Semester

Course Code:CE-406					        Duration:1 hour

Course Name: Concrete Technology Lab		     Max.Marks:20 Marks

----------------------------------------------------------------------------------------------------------------

Instructions to the Candidate:

(i)Answer any One of the following Questions.Each question carries 20 marks

(ii) Check the suitability of the given construction material by drawing suitable inference

- Determine workability of the fresh concrete prepared with the given mix proportion and water cement ratio using slump test

- Determine the compaction factor of the fresh concrete prepared with the given mix proportion and water cement ratio using compaction factor test

- Determine the workability of freshly mixed concrete by using of Vee – Bee consistometer

State Board of Technical Education and Training, Telangana

Semester End Examination

Model Question paper

DCTMIV Semester

Course Code:CE-406					        Duration:2 hours

Course Name: Concrete Technology Lab		  Max.Marks:40 Marks

----------------------------------------------------------------------------------------------------------------

Instructions to the Candidate:

(i)Answer any One of the following Questions.Each question carries 40 marks

(ii) Check the suitability of the given construction material by drawing suitable inference

- Calculate the impact value of given sample of coarse aggregate

- Calculate the crushing value of given sample of coarse aggregate

- Calculate the abrasion value of given sample of coarse aggregate

- Calculate the flakiness index of given sample of coarse aggregate

- Calculate the elongation index of given sample of coarse aggregate

- Determine workability of the fresh concrete prepared with the given mix proportion and water cement ratio using slump test

- Determine the compaction factor of the fresh concrete prepared with the given mix proportion and water cement ratio using compaction factor test.

- Determine the workability of freshly mixed concrete by using of Vee – Bee consistometer

- Prepare three sample concrete cubes with the given mix proportion and water cement ratio

- Calculate the compressive strength of the given cement concrete cubes

- Calculate the compressive strength of the given cement concrete cylinder

- Determine the Flexural Strength of Concrete